Material Safety / Data Sheet

I. General Information

Chemical Name & Synonyms			     Trade Name & Synonyms

Modified Oxychloride Cement			      AirKrete Insulation

Chemical Family					     Formula

Calcium, Magnesium oxide, Alumina		      Proprietary

Proper DOT Shipping Name			     DOT Hazard Classification

Manufacturer					     Manufacturer’s Phone Number

Air Krete, Inc.						      (315) 834-6609

PO Box 380

Weedsport, NY 13166-0380

II. Ingredients

Principal Hazardous Components - Percent 	   Threshold Limit Value (units)

Non-Hazardous				N/A		    N/A

III. Physical Data

Boiling Point (°F) 				Specific Gravity (H20=1)

N/A							2.0 lbs approximate per cubic foot

Thermal Resistance				Shrinkage

K-factor at 75°F – 0.257				Shrinkage 0

R-factor – 3.9 per inch				Shrinkage Percent 0

Closed Cavity – 0.00 ASTMC 951

Vapor Pressure (mmHg.) 	           	Percent Volatile by Volume (%)

N/A					            	 Non-volatile

No Formaldehyde or organic vapors

Vapor Density (Air = 1)		           	Evaporation Rate (____ = 1)

N/A

Solubility in Water pH				Appearance & Odor

Light green in color.					Odorless Insoluble 	10.5 – 11.0

IV. Fire & Explosion Hazard Data

Flash Point Test					Auto Ignition Temperature

N/A							Non-combustible

Flammable Limits

N/A

Extinguishing Media				LEL			UEL

N/A							N/A			N/A

Special Fire Fighting Procedures

N/A

Unusual Fire & Explosion Hazards

Non-combustible	ASTM E-84

Flame Spread – 0, Smoke Developed – 0, Fuel Contributed – 0

(Test extended to 30 minutes)

V. Data Health Hazard

OSHA Permissible Exposure Limit		ACGIH Threshold Limit Value

N/A							N/A

Carcinogen NTP Program			Carcinogen IARC Program

N/A							N/A

Symptoms of Exposure

None Known

Primary Route(s) of Entry

N/A

Emergency First Aid

N/A

VI. Reactivity Data

Stability						Unstable Conditions to Avoid

Stable							N/A

Incompatibility 					Materials to Avoid

N/A							N/A

Hazardous Polymerization May Occur	Conditions to Avoid

Will not occur						N/A

Hazardous Decomposition Produces

None

VII. Environmental Protection Procedures

Spill Response

N/A

Waste Disposal Method:	This product is considered non-hazardous as waste charged by an analytical parameters using EPA methods or standard measure per 15th edition and AEP toxicity. Normal landfill – Report dated 1/10/84, file #405.030, sample #12183.

VIII. Special Protection Procedures

Eye Protection					Skin Protection

N/A							(Gloves – optional)

Respiratory Protection (Special Type)	Ventilation Recommended

N/A							Dust mask

Other Protection

N/A

IX. Special Precautions

Hygienic Practices in Handling & Storage

N/A

Precautions for Repair & Maintenance of Contaminated Equipment

N/A

Other Precautions

N/A

©2011 AirKrete®, Inc.

Revision Date:  2011